## Slide 1
Optimization of Co addition amount to enhance thermoelectric properties of β-FeSi2
Sopheap Sam1,*, Genki Kashikawa1, Hiroshi Nakatsugawa1, Yoichi Okamoto2
Yokohama National University, Japan
National Defense Academy, Japan
* E-mail: sam-sopheap-fh@ynu.jp
2022-March-24

## Slide 2: Outline
Introduction
- Crystal and band structure FeSi2.
- Phase transition of FeSi2.
- Review of previous researches.
- Strategy to improve TE performance of β-FeSi2.
2. Experimental method
- Fabrication and measurement.
3. Results and discussions
- Phase transition of FeSi2 and crystal structure.
- Thermoelectric properties (Seebeck coefficient, electrical resistivity, thermal conductivity, and ZT).
4. Conclusions

## Slide 3
Crystal and band structure of each phase FeSi2
Orthorhombic β-phase
Tetragonal α-phase
Cubic ε-phase
Space group: P213
Space group: P4mmm
Space group: Cmca
R. Girlanda et al., J. Appl. Phys. 76, 2837 (1994)
S. J. Clark et al., Physical review B., 58,16 (1998)
Fe1
Fe2
Si1
Si2

## Slide 4
Phase transition diagram of FeSi2
The equilibrium phase diagram for the system Fe–Si by Piton and Fay. α-phase:FeSi2, β-phase:FeSi2, ε-phase:FeSi.
The β-FeSi2 based material is a promising candidate for thermoelectric (TE) application working at high temperatures up to 900 oC due to:
Environmental friendliness
Good thermal stability
Strong oxidation resistance
Low cost.
[X. L. Du et al., Acs Applied Materials & Interfaces, 12, 12901-12909 (2020)]

## Slide 5
Review of previous researches
ZTmax = 0.085 at 657 K of Fe0.95Co0.05Si2 by pressure sintering method.
ZTmax = 0.25 at 940 K of Fe0.95Co0.05Si2 by spark plasma sintering method.
[S. W. Kim et al., Intermetallics, 11, 399-405 (2003)]
[J. Tani and H. Kido, Japanese Journal of Applied Physics, 40, 3236-3239 (2001)]
S: Seebeck coefficient [V/K]
ρ: resistivity [Ω.m]
κ: thermal conductivity[W/m.K]

## Slide 6
Strategy to improve TE performance of β-FeSi2 by Co doping
Resistivity (ρ) can be decreased by the increase in carrier density (nH) by Co-doing due to the larger valence electron.
However, with increasing x, as decreasing the ρ, the Seebeck coefficient |S| also decreases. Therefore, we need to find the optimum Co doping and carrier density in β-Fe1-xCoxSi2 .
Seebeck coefficient (S) :
large me*
small mh*
mobility
In β-FeSi2 (x=0), the Seebeck coefficient |S| decreases with increasing temperature because of the bipolar effect.
By Co doping, Hall mobility μH decreases and |S| increases because of the majority carrier for electrons.

## Slide 7
Arc-melting (20g)
NC wire cut
7x7x1.5mm
Vacuum sealing in quartz tube
Heat treatment 1150 oC, 3h
Annealing
840 oC, 20h
Experimental method
Fabrication :
7x7x1.5mm
Furnace 1150 oC, 3h.
Furnace 840 oC, 20 h.
Measurement :
XRD by Smart Lab, Rigaku
Rietveld analysis by RIETEN-FP
Thermal conductivity by power efficiency measurement (PEM-2)
ZT calculated by above parameters
Carrier concentration and mobility at RT by ResiTest 8300
Resistivity and Seebeck coefficient by ResiTest 8300 and homemade apparatus

## Slide 8
x=0.00
x=0.03
x=0.06
x=0.07
x=0.10
(202)
(312)
(221)
(331)
(422)
(024)
(242)
(602)
(533)
(515)
β-phase
β-phase
β-phase
α+β-phase
α, (312)
α, (312)
x=0.005
x=0.01
x=0.015
x=0.02
x=0.04
β-phase
β-phase
β-phase
β-phase
β-phase
β-phase
x=0.05
α+β-phase
x=0.08
α, (312)
x=0.09
Intensity / arb.unit
(112)
(515)
(533)
(602)
(242)
(024)
(422)
(331)
(221)
(312)
(202)
(112)
α+β-phase
α+β-phase
α, (312)
Intensity /arb.unit
Diffraction angle, 2θ / degree
Diffraction angle, 2θ / degree
Phase transition
The α phase (metallic phase) is grown from x=0.07 sample. This phase is not good for TE application.
∆V is low in metallic phase.
X-ray diffraction patterns of Fe1-xCoxSi2 (0 ≤ x ≤ 0.10) at room temperature

## Slide 9
Crystal structure identification by Rietveld analysis
By using Rietveld Analysis with the measured data of XRD, all samples were grown in single beta β phase crystal structure with Cmca space group (base-centered orthorhombic) after heat treatment 1150 oC 3 h and annealing 840 oC 20 h.
FeSi2
β-FeSi2
(221)
(312)
(331)
(202)
(422)
(242)
(602)
(533)
(515)
(024)
(112)
Si2
Si1
Fe2
Fe1
a
b & c

## Slide 10
As Co addition increases, the ρ significantly decreases due to high nH.
At 300K, the |S| of 0.005 ≤ x ≤ 0.06 samples are in range 371-145 μV/K which is higher than 127 μV/K of x = 0 .
Electrical resistivity (ρ) and Seebeck coefficient (S) of β-Fe1-xCoxSi2
Bipolar effect deteriorates S due to narrow band gap.

## Slide 11
Thermal conductivity (κ) of β-Fe1-xCoxSi2
The high values of κ are found in x=0.005, while the minimum values of that are obtained in x=0.04. The κ slightly decreases with Co addition.

## Slide 12
ZTmax
The highest ZT of non-doped β-FeSi2 is only about 2.6 × 10-4 at 450K.
ZTmax = 0.099 at 720-800 K is obtained in x=0.03 with the optimum nH =1.2(4) × 1020 cm-3 and μH= 3.5(6) cm2.V-1.s-1.
The improvement of ZT in Co-doped samples is due to the significant enhancement in PF and also the slight reduction in κ.
Thermoelectric performance (ZT) of β-Fe1-xCoxSi2

## Slide 13
Conclusions
The thermoelectric (TE) materials β-Fe1-xCoxSi2 (0 ≤ x ≤ 0.06) have been successfully fabricated and TE properties were measured.
The |S| of all Co doping samples is higher than that of non-doping sample due to the absence of bipolar effect with the lower electrons mobility.
The |S| and ρ simultaneously decrease with increasing Co addition due to the increase in nH.
The highest ZT = 0.099 at 720-800 K is obtained in optimum point x = 0.03 with the nH around 1.2(4) × 1020 cm-3.
Authors | ZTmax | x | Temperature [K] | Fabrication method
J. Tani and H. Kido | 0.25 (higher S) | 0.05 | 940 | Spark plasma sintering
S. W. Kim et al. | 0.085 (lower S) | 0.05 | 657 | Pressure sintering
This study | 0.099 | 0.03 | 720-800 | Arc melting

## Slide 14: Thank you for your attention!

## Slide 15
TE properties at RT
x | L𝚶 [V2/K2] | r | nH [1/cm3] | μH [cm2/V.s ] | ¦S¦ [μV/K] | ρ [Ω.cm] | κ [W/mK]
0 | 1.792×10-8 | -1/2 | 6.3(9)×1016 | 14(2) | 127 | 7.23(7) | 7.16
0.005 | 1.625×10-8 | -1/2 | 9.3(0)×1018 | 6.1(3) | 371 | 0.108(0) | 8.97
0.01 | 1.625×10-8 | -1/2 | 1.8(0)×1019 | 5.4(2) | 357 | 0.063(0) | 6.72
0.015 | 1.627×10-8 | -1/2 | 2.8(4)×1019 | 5.2(8) | 299 | 0.043(0) | 6.82
0.02 | 1.628×10-8 | -1/2 | 1.0(8)×1020 | 4(2) | 287 | 0.027(1) | 6.30
0.03 | 1.644×10-8 | -1/2 | 1.2(4)×1020 | 3.5(6) | 213 | 0.015(0) | 6.33
0.04 | 1.671×10-8 | -1/2 | 1.3(0)×1020 | 2.4(0) | 179 | 0.019(0) | 5.14
0.05 | 1.688×10-8 | -1/2 | 2.5(3)×1020 | 2.4(4) | 167 | 0.010(0) | 5.18
0.06 | 1.735×10-8 | -1/2 | 4.2(8)×1020 | 1.9(4) | 145 | 0.008(0) | 5.26

## Slide 16
Power factor (PF) of β-Fe1-xCoxSi2
The highest PF value of non-doped sample is only around 3.4 μW.m-1. K-2 at 450K.
By doping with Co, the PF was significantly enhanced.
The optimum doping x=0.03 with the maximum value of around 900 μW.m-1. K-2 at 720-800K
PFmax

## Slide 17
Bipolar
Bipolar effect remarkably dominate at low nH .
J. J. Gong et al., Physical Chemistry Chemical Physics,18, 16566-16574 (2016).