## Slide 1
Thermoelectric properties of bulk Ni-doped 𝛃-FeSi2
Sopheap Sam1, *, Soma Odagawa1, Hiroshi Nakatsugawa1, Yoichi Okamoto2
2023-March-16th
Yokohama National University, Japan
National Defense Academy, Japan
* E-mail: sam-sopheap-fh@ynu.jp

## Slide 2: Content
Introduction
- Crystal and band structure FeSi2.
- Phase transition of FeSi2.
- Review of previous research.
- Improve thermoelectric(TE) performance of β-FeSi2 by Ni substitution.
2. Experimental method
- Fabrication and measurement.
3. Results and discussion
- Crystal structure and phase identification.
- TE properties (Seebeck coefficient, electrical resistivity, thermal conductivity, and ZT).
4. Conclusions

## Slide 3
1. Introduction

## Slide 4
Crystal Structure of each phase FeSi2
Orthorhombic β-phase
Tetragonal α-phase
Cubic ε-phase
Space group: P213
Space group: P4mmm
Space group: Cmce
R. Girlanda et al., J. Appl. Phys. 76, 2837 (1994)
S. J. Clark et al., Phys. Rev. B., 58,16 (1998)

## Slide 5
Phase transition diagram of FeSi2
The equilibrium phase diagram for the system Fe–Si by Piton and Fay. α-phase:FeSi2, β-phase:FeSi2, ε-phase:FeSi.
The β-FeSi2 based material is a promising candidate for thermoelectric (TE) application working at high temperatures due to:
Environmental friendliness
Good thermal stability
Strong oxidation resistance
Low cost.
X. L. Du et al., Acs Appl. Mater. Interfaces, 12, 12901-12909 (2020).
J. P. Piton and M. F. Fay, C. R. Acad. Sci. (Paris). C266, 514–516 (1968).

## Slide 6
Review of previous research
S: Seebeck coefficient [V/K]
ρ: resistivity [Ωm]
κ: thermal conductivity[W/mK]
β-Fe1-yNiySi2
β-Fe0.99-yCo0.01NiySi2
Smax at Ni doping 0.01
J. Tani and H. Kido J. Appl. Phys., 84, 1408-1411 (1998).
H. Nagai et. al., J. Jpn. Soc. Powder Powder Metall., 41, 560-564, 1994.
ρ can be reduced due to an increase in carrier concentration.
S can be increased by Ni substitution probably due to a reduction in mobility.

## Slide 7
Improve TE performance of Ni doping Fe1-xNixSi2
Resistivity (ρ):
Find the optimum Ni doping to improve the performance of β-FeSi2!
Seebeck coefficient (S) :
large me*
small mh*
Mobility
In pure β-FeSi2 (x=0), the Seebeck coefficient |S| decreases with increasing temperature because of the bipolar effect.
By Ni doping, Hall mobility μH decreases and |S| increases because of the majority carrier are electrons.
; Ni valence electron = 2 Fe.

## Slide 8
Research purpose:
Investigate the thermoelectric properties of Ni-doped β-FeSi2 prepared by the direct arc melting method.
Study the effect of Ni on the solid solution limit and phase transition of β-FeSi2.
Find the optimum doping concentration of Ni substitution to improve thermoelectric properties.
Komabayashi et al. Jpn. J. Appl. Phys. ,30, 1906 (1991).
Nagai et al. J. Jpn. Soc. Powder Powder Metall. 41, 560 (1994).
Power factor of Ni-doped β-FeSi2 of previous research:

## Slide 9
2. Experimental method

## Slide 10
Arc-melting (20g)
NC wire cut
7x7x1.5mm
Vacuum sealing in quartz tube
Heat treatment 1150 oC, 3h
Annealing
840 oC, 20h
Fabrication :
7x7x1.5mm
Furnace 1150 oC, 3h.
Furnace 840 oC, 20 h.
Measurement :
XRD by Smart Lab, Rigaku
Rietveld analysis by RIETEN-FP
Thermal conductivity by power efficiency measurement (PEM-2)
ZT calculated by above parameters
Carrier concentration and mobility at RT by ResiTest 8300
Resistivity and Seebeck coefficient by ResiTest 8300 and homemade apparatus
3D SEM VE-8800
Ohtaki et al., Chem. Lett. 22, 1067-1070 (1993).
This annealing condition was optimized by Ohtaki et al., for Cu, Zn, Nb, Ag, and Sb doping.

## Slide 11
3. Results and discussion

## Slide 12
X-ray diffraction patterns and SEM images of non-doped FeSi2 (x = 0)
Before heat treatment
After heat treatment
ε + α phases.
Non-doped, x = 0.
β + ε phases.
Non-doped, x = 0.
Heat treatment at:
1150 oC, 3h
840 oC, 20h
Before
After
Indexed peaks are β-phases

## Slide 13
X-ray diffraction patterns and SEM images of Fe1-xNixSi2 at room temperature

## Slide 14
Elemental analysis by SEM-EDS at room temperature
The ε-phase increases with Ni substitution and solid solution limits of Ni in β-FeSi2 can be lower than 1%.

## Slide 15
Electrical resistivity (ρ) of β-Fe1-xNixSi2
x
nH
ρ
μH
ρ
The increase in nH contributes positively to the decrease in ρ.
The decrease in μH contributes negatively to the decrease in ρ.

## Slide 16
x
Seebeck coefficient (S) of β-Fe1-xNixSi2
x=0, bipolar effect deteriorates S.
nH
|S|
The bipolar effect is reduced by Ni substitution
|S|max

## Slide 17
Solid lines are the calculated data at various effective masses (m*) using Mott’s equation:
Various shape plots are the experimental data.
A good fitting condition is obtained at m* = 0.12me.
Seebeck coefficient vs carrier density at room temperature
The Ni-doped sample has an effective mass of 0.12me, mobility of about 10 - 40 cm2V-1s-1, and relaxation time of about 0.68 fs - 2.73 fs.

## Slide 18
Thermal conductivity (κ) and ZT of β-Fe1-xNixSi2
The κ of Ni doping samples is higher than that of non-doped samples probably due to the increase in nH.
ZTmax
The ZTmax = 0.019 is obtained in the x = 0.001 sample due to the significant increase of S and also the decrease in resistivity.

## Slide 19
4. Conclusion

## Slide 20
Conclusions
The electrical resistivity decreases with Ni doping level due to an increase in nH.
The Seebeck coefficient decrease with Ni doping level, where the highest value is obtained in x = 0.001 with the value of 450 μV/K at 450 K. Small doping amount is more effective.
The thermal conductivity slightly increases with Ni doping.
The highest ZT = 0.019 at 600 K is obtained in the x = 0.001 sample due to the significant increase in the Seebeck coefficient and reduction in electrical resistivity.
Authors | x | S [μV/K] | PF [μW/mK2] | Fabrication method
Komabayashi et al. at 300K | 0.06 | -113 | 17 | Thin film by RF sputtering
This study at 300K | 0.001 | -393 | 13 | Bulk by arc melting
Nagai et al. at 650K | 0.01 | -190 | 50 | Bulk by mechanical milling + hot-pressing
This study at 600K | 0.001 | - 450 | 280 | Bulk by arc melting

## Slide 21
For more details, please refer to the full paper in the Materials journal:
Thank you for your kind attention!

## Slide 22: Appendix

## Slide 23
Crystal structure and phase identification by Rietveld analysis
The samples were grown in β-phase crystal structure with Cmce space group (base-centered orthorhombic) after heat treatment 1150 oC 3 h and annealing 840 oC 20 h.
Si2
Si1
Fe2
Fe1
A small amount of ε-phase at 2θ=45.2 deg.

## Slide 24
Power factor (PF) of β-Fe1-xNixSi2
PFmax
PF of x = 0.001 is about 60 times higher than that of x = 0.

## Slide 25
β-Fe1-xNixSi2
β-Fe1-xCoxSi2
S of Co-doped samples are more uniform with temperature
S of Ni-doped samples are less uniform with temperature.
ρ of Co-doped samples are uniform with temperature.
ρ of Ni-doped samples remarkably decreases at high temperature.
Role of each dopant:
- Co: stabilize small ρ and large S with increasing temperature because of large nH and large m*, respectively.
- Ni: decrease ρ @ high temperature probably due to increase μH with increasing temperature.
Result: More improved PF.
Future research for co-doping of Co+Ni

## Slide 26
TE properties of β-Fe1-xNixSi2 at RT
x | L𝚶 [V2/K2] | r | nH [1/cm3] | μH [cm2/V.s ] | ¦S¦ [μV/K] | ρ [Ω.cm] | κ [W/mK] | Relative density [%]
0 | 1.792×10-8 | -1/2 | 2.3(2)×1016 | 37(4) | 127 | 7.10 | 7.16 | 98.0(1)
0.001 | 1.624×10-8 | -1/2 | 1.2(4)×1017 | 35(7) | 393 | 1.39 | 8.25 | 98.3(1)
0.005 | 1.656×10-8 | -1/2 | 2.6(2) ×1017 | 34(3) | 194 | 0.69 | 8.57 | 96.24(8)
0.010 | 1.648×10-8 | -1/2 | 3.2(7) ×1017 | 27(5) | 205 | 0.69 | 8.44 | 97.5(3)
0.015 | 1.674×10-8 | -1/2 | 4.8(4) ×1017 | 20(1) | 176 | 0.63 | 7.27 | 98.7(1)
0.02 | 1.766×10-8 | -1/2 | 1.2(4) ×1018 | 11(3) | 135 | 0.45 | 7.12 | 95.6(2)
0.03 | 2.139×10-8 | -1/2 | 2.3(2) ×1018 | 10(1) | 62 | 0.26 | 6.18 | 95.6(1)

## Slide 27
Si2
Si1
Fe2
Fe1

## Slide 28
Lattice parameter of β-Fe1-xNixSi2 at RT

## Slide 30
Bipolar
Bipolar effect remarkably dominate at low nH .
J. J. Gong et al., Physical Chemistry Chemical Physics,18, 16566-16574 (2016).