## Slide 1
Thermoelectric properties of β-FeSi2 with Co and Ni addition
1
Sopheap Sam 1, Hiroshi Nakatsugawa1, *, Yoichi Okamoto 2
1 Yokohama National University, 2 National Defense Academy
* E-mail : nakatsugawa-hiroshi-dx@ynu.ac.jp
2023/09/22

## Slide 2: Contents
Introduction
Crystal and band structure FeSi2
Phase transition of FeSi2
Review of previous research
Research purpose
Experimental methods
Fabrication
Measurement
Results and discussion
Crystal structure
Microstructure
Electrical properties
Thermoelectric properties
Conclusions
Summary
Future issue

## Slide 3
Introduction
3

## Slide 4
Crystal Structure of each phase FeSi2
Orthorhombic β-phase
Tetragonal α-phase
Cubic ε-phase
Space group: P213
Space group: P/4mmm
Space group: Cmce
R. Girlanda et al., J. Appl. Phys. 76, 2837 (1994)
S. J. Clark et al., Phys. Rev. B., 58,16 (1998)

## Slide 5
Phase transition diagram of FeSi2
The equilibrium phase diagram for the system Fe–Si by Piton and Fay. α-phase:FeSi2, β-phase:FeSi2, ε-phase:FeSi.
The β-FeSi2 based material is a promising candidate for thermoelectric (TE) application working at high temperatures due to:
Environmental friendliness
Good thermal stability
Strong oxidation resistance
Low cost.
X. L. Du et al., Acs Appl. Mater. Interfaces, 12, 12901-12909 (2020).
J. P. Piton and M. F. Fay, C. R. Acad. Sci. (Paris). C266, 514–516 (1968).

## Slide 6
β-Fe1-xNixSi2
S of Co-doped samples are more uniform with temperature
S of Ni-doped samples are less uniform with temperature.
- Co: stabilize small ρ and large S with increasing temperature because of large nH and large m*, respectively.
- Ni: decrease ρ at high temperature probably due to increase μH with increasing temperature.
Co+Ni: More improved PF.
Previous studies
β-Fe1-xCoxSi2
m* = 6.0me ,
μH = 4 cm2V-1s-1
τ =13.6 fs
m* = 0.12me
μH = 10-40 cm2V-1s-1
τ = 0.68 fs - 2.73 fs
Sam et al., Jpn. J. Appl. Phys. 61, 111002 (2022)
Sam et al., Materials. 16, 927 (2023)

## Slide 7
Study the effects of Co and Ni on the structure and phase transition of β-Fe0.97-xNixCo0.03Si2 prepared by the arc melting method.
Investigate the electrical and thermoelectric properties of Co and Ni-doped β-FeSi2 prepared by the arc melting method.
Find the optimum doping concentration of Co and Ni substitution to optimize carrier density and mobility for improving electrical and thermoelectric properties.
Objective of research

## Slide 8
Experimental methods

## Slide 9
Arc-melting (20g)
NC wire cut
7x7x1.5mm
Vacuum sealing in quartz tube
Heat treatment 1150 oC, 3h
Annealing
840 oC, 20h
Fabrication :
7x7x1.5mm
Furnace 1150 oC, 3h.
Furnace 840 oC, 20 h.
Measurement :
XRD by Smart Lab, Rigaku
Rietveld analysis by RIETEN-FP
Thermal conductivity by power efficiency measurement (PEM-2)
ZT calculated by above parameters
Carrier concentration and mobility at RT by ResiTest 8300
Resistivity and Seebeck coefficient by ResiTest 8300 and homemade apparatus
3D SEM-EDS by VE-8800 & SU8010
Ohtaki et al., Chem. Lett. 22, 1067-1070 (1993).
This annealing condition was optimized by Ohtaki et al., for Cu, Zn, Nb, Ag, and Sb doping.

## Slide 10
Results and discussion

## Slide 11
X-ray diffraction patterns and SEM images of non-doped FeSi2 (x = 0)
Before heat treatment
After heat treatment
ε + α phases.
Non-doped, x = 0.
β + ε phases.
Non-doped, x = 0.
Heat treatment at:
1150 oC, 3h
840 oC, 20h
Before
After
Indexed peaks are β-phases

## Slide 12
Rietveld analysis of Fe0.97-xNixCo0.03Si2 at room temperature
A trace of the ε-phase is contained in all samples.
The peak of the ε-phase increase with increasing Ni contents.

## Slide 13
Microstructure and phase fraction of Fe0.97-xNixCo0.03Si2
The grain of the ε-phase increase with Ni.
ε-phase is more dominant than α-phase.
Orthorhombic phase changes to cubic phase.
Because the atomic size of Ni is smaller than Fe.

## Slide 14
Elemental analysis by SEM-EDS of Fe0.97-xNixCo0.03Si2 at room temperature
The ε-phase increases with Ni substitution and solid solution limits of Ni in β-FeSi2 can be lower than 1%.
The Co distribution becomes less homogeneous with increasing Ni content.

## Slide 15
Ni decreases the solubility of Co.
Ni has a lighter effective mass (m*).
Ni has a lighter m*.
Increase nH
Increase μH
Increase ε-phase.
Electrical resistivity (ρ) and Seebeck coefficient (S) of β-Fe0.97-xNixCo0.03Si2

## Slide 16
Seebeck coefficient vs carrier density at room temperature β-Fe0.97-xNixCo0.03Si2
Solid lines are the calculated data at various effective masses (m*) using Mott’s equation:
Various shape plots are the experimental data.
A good fitting condition is obtained at m* = 0.9me.
The Ni-doped sample has an effective mass of 0.9me, mobility of about 25 cm2V-1s-1, and relaxation time of about 12.8 fs.

## Slide 17
Thermal conductivity (κ) and ZT of β-Fe0.97-xNixCo0.03Si2
The κ slightly decreases with Ni probably due to the increase in pores.
Pores
The ZTmax = 0.31 at 720 K is obtained in the x = 0.01 sample due to the reduction in ρ with higher μH.

## Slide 18
Conclusions

## Slide 19
Summary
The electrical resistivity decreases with Ni addition due to the increased mobility.
The Seebeck coefficient decreases with Ni doping level due to the formation of ε-phase.
The thermal conductivity slightly decreases with Ni doping because of porosity.
The highest ZT = 0.31 at 720 K is obtained in the x = 0.01.
Authors | Dopant | Maximum ZT | Fabrication method
Abbassi et al. at 723 K 1) | Co 5% | 0.14 | Spark plasma sintering
Kim et al. at 845 K 2) | Co 5% +Ge 2% | 0.11 | Pressuring sintering
Du et al. at 900 K 3) | Co 6% +Ru 5% | 0.33 (low κ) | Pressure sintering
This study at 720 K | Co 3% +Ni 1% | 0.31 | Arc melting
Abbassi et al., Nanomaterials 11, 2852 (2021).
Kim et al., Intermetallics 11, 399 (2003).
Du et al., ACS Appl. Mater. Interfaces 11, 32151 (2019).
Future issue
The thermal conductivity could be further reduced by alloying with heavy elements or the nanostructuring techniques.

## Slide 20: Thank you for your kind attention!
For more details, please refer to our full paper published in Materials Advances journal!
S. Sam, H. Nakatsugawa, and Y. Okamoto, Mater. Adv. 2023, 4, 2821-2830.

## Slide 21
Appendix A
of Co doping <
m*Co > m*Ni
Co-doped sample
m* = 6.0me ,
μH = 4 cm2V-1s-1
τ =13.6 fs
Ni-doped sample
m* = 0.12me
μH = 10-40 cm2V-1s-1
τ = 0.68 fs - 2.73 fs
Energy, E
Wave number, k
Conduction band
Valence band
Co doping
Ni doping
of Co doping
of Ni doping
Effective mass depends on band structure for Co and Ni-doped FeSi2
of Ni doping

## Slide 22
Bipolar = 2 poles
Negative pole (electron, e-)
Positive pole (hole, h+)
e-
e-
e-
h+
h+
Valence band
Conduction band
Low temperature
High temperature
Low carrier density, nH
Se-
Sh+
Se- > Sh+
Se- ≈ Sh+
Total Seebeck, STotal = - Se- + Sh+ = -S
e-
e-
h+
h+
Sh+
Se-
e- & h+ are mixed/ excited.
STotal = - Se- + Sh+ ≈ 0
High carrier density, nH
ne- ≈ nh+
e-
e-
e-
h+
h+
Valence band
Conduction band
Low temperature
High temperature
Se-
Se-≫ Sh+
Se- ≫ Sh+
e-
e-
h+
h+
Se-
e-
e-
e-
e-
ne- ≫ nh+
Sh+
Sh+
STotal = - Se- + Sh+ = -S
STotal = - Se- + Sh+ = -S
Non-doped FeSi2
Co and Ni-doped FeSi2
Decrease Seebeck
Uniform Seebeck
large me*
small mh*
mobility
bipolar effect
Seebeck coefficient
Appendix B

## Slide 23
Ni concentration (x)
Appendix C
Lattice constants
Power factor (PF)