## Slide 1
Self-cooling on power MOSFET using n-type Si wafer
H.Nakatsugawa, T.Sato, Y.Okamoto, T.Kawahara, and S.Yamaguchi
E-mail : naka@ynu.ac.jp
Yokohama National University,
National Defense Academy,
Chubu Uiversity
ECT2011 Sep. 28-30, 2011 – Thessaloniki, GREECE
Notes: Today I would like to talk about “Self-cooling on power MOSFET using n-type Si wafer”. My name is Hiroshi Nakatsugawa from Yokohama National University.

## Slide 2
The n-type Si wafer is one of the candidate materials for use to cool down the power devices both by the thermal conduction and by the Peltier effect.
Notes: This is the take home message that the n-type Si wafer is one of the candidate materials for use to cool down the power devices both by the thermal conduction and by the Peltier effect.

## Slide 3
Metal Oxide Semiconductor Field Effect Transistors
Insulated Gate Bipolar Transistors
Central Processing Units
Gate
Gate
Emitter
Collecter
Drain
Source
silicon power devices
Notes: I’m going to begin my talk by giving you a brief background of power devices. As you know, silicon power devices that include power MOSFET, IGBT and CPU are used in a daily life. When we use these devices, the improvement of heat removal or cooling is one of the most important issues because they will not function correctly above 150℃.

## Slide 4
power device cooling
CPU cooling
power device
CPU
fin
fin
fan
heat dissipation
Peltier heat dissipation
Peltier module
Notes: There are three different ways to remove the heat from power devices. One is to use fin connected with power devices. This cooling system uses only thermal conduction. But the size of fin is larger than that of power device. The second way is to use Peltier module connected with large fin and fan. This cooling system uses only Peltier heat flux. However, the electric power consumption will be increased because Peltier module, fan and power devices need different DC power supplies for each operation.

## Slide 5
current
current
Conventional cooling system
Self-cooling device
power MOSFET (IRF1324PbF)
RDS(On)=1.5mΩ (VGS=10V, ID<195A)
D
S
S
G
G
D
D
60A
6W
60A
1.5cm
3cm
520μm
copper plating n-type Si wafer
Joule heat @60A = 0.94W
7～8W
n-type TE materials
power devices
Notes: The third way is to use self-cooling device proposed by Yamaguchi et al. in four years ago. This cooling system applies both thermal conduction and Peltier heat by using self-current in this device. The point is that this cooling system consists of n-type thermoelectric material connected to drain for the power MOSFET.

## Slide 6
a high Seebeck coefficient
a high electrical conductivity
a high thermal conductivity
The purpose of this study is to develop the self-cooling device using n-type thermoelectric material and to estimate the heat flux both by thermal conduction and by Peltier effect.
Notes: The purpose of this study is to develop the self-cooling device using n-type thermoelectric material and to estimate the heat flux both by thermal conduction and by Peltier effect. It is necessary that thermoelectric materials for self-cooling device have not only a high Seebeck coefficient and a high electrical conductivity but also a high thermal conductivity. So, for example, single crystal silicon must be one of the candidate materials for self-cooling device.

## Slide 7
electric resistivity of n-type Si
Seebeck coefficient of n-type Si
SEM image of copper plating Si
EPMA micrographs of copper plating Si
1μm
Ti
0.1μm
1μm
Au
0.4μm
Cu plate
Si
1μm
Notes: In fact, the commercial n-type silicon wafer was used for self-cooling device because of a low electrical resistivity and a high Seebeck coefficient. The n-type silicon wafer was coated on both surfaces with 0.1 micro meter of titanium to endure adhesion and 0.4 micro meter of gold, deposited by sputtering. The electrodes were fabricated on both surfaces with a thickness of about 2 micro meter deposited by copper plating.

## Slide 8
CA-1112 (EYELA)
VGS=10V
ID=60A
water cooled heatsink
8
TVS-200EX (NEC Avio )
D
S
S
G
G
D
D
1.5cm
3cm
520μm
upper side
Notes: The power MOSFET and the copper plating n-type silicon wafer were located between upper and lower copper block. In this system, the electric current of 60A flowed from lower to upper direction. The water temperature of the heatsink was maintained about 4℃ constantly by the cooling water circulation system. To determine whether the self-cooling device remove the heat from the power MOSFET, we studied the time dependence of the temperature distribution by using the infra-red thermography.

## Slide 9
current
60A
6W
30 minutes
32.9℃
40 minutes
50 minutes
32.7℃
Joule heat
32.4℃
33.4℃
60 minutes
Notes: These figures show the temperature distribution of Joule heat from power MOSFET after 30, 40, 50 and 60 minutes. The temperature distributions of the upper side are in the range 27 to 36℃. In particular, the temperature distributions show the peak of the pixel value at about 33℃. This means that the average temperature of the upper side in this system is about 33℃. This figure shows the time dependence of the Joule heat and the input power. The Joule heat is measured 6W constantly, and also the input power is measured 48W constantly.

## Slide 10
current
60A
7～8W
32.2℃
30 minutes
32.2℃
40 minutes
32.9℃
50 minutes
Joule heat
Peltier heat
60 minutes
32.4℃
Notes: These figures show the temperature distribution of the Joule heat from power MOSFET with the n-type silicon wafer after 30, 40, 50 and 60 minutes. The temperature distributions show the peak of the pixel value at about 32℃. In particular, the increase of the input power and the output power is about 4W constantly. It is assumed that both the Joule heat and the Peltier heat generate, so that the heat removal can be explained reasonably. If the increase of 4W is due to the Joule heat, the temperature distribution should be enhanced higher temperature. Therefore, the Peltier heat should make a contribution to cool down the power MOSFET with n-type silicon wafer.

## Slide 11
summary
The self-cooling device was developed and was estimated heat flux both by thermal conduction and by Peltier effect.
The average temperature of upper side of power MOSFET was cooled down by addition of the n-type Si wafer.
The n-type Si wafer is one of the candidate materials for use in the self-cooling device.
Notes: To summarize, we developed the self-cooling device and estimated heat flux both by thermal conduction and by Peltier effect. We revealed that the average temperature of upper side of power MOSFET was cooled down by addition of the n-type Si wafer. We conclude that the n-type Si wafer is one of the candidate materials for use in the self-cooling device.

## Slide 12
Thank you for your kind attention.
Acknowledgements
Notes: Thank you for your kind attention.

## Slide 13
current
60A
6W
2A
2.6V
30 minutes
31.3℃
40 minutes
32.8℃
50 minutes
33.8℃
60 minutes
35.0℃
Introduction
Peltier module (KSM-06071C)
Imax=6A, Vmax=8.3V
2A
2.6V
27℃
7 ℃
8W
13W

## Slide 14
Peltier module (KSM-06071C)
Imax=6A, Vmax=8.3V
2A
2.5V
27℃
7 ℃
8W
13W
6A
8V
27℃
7 ℃
20W
68W

## Slide 15
60A
14.6℃
30 minutes
14.6℃
40 minutes
15.7℃
50 minutes
14.1℃

## Slide 16
60A
1～2W
30 minutes
16.7℃
40 minutes
13.1℃
50 minutes
13.1℃
Joule heat
Peltier heat

## Slide 17
current
60A
2A
2.6V
30 minutes
40 minutes
50 minutes
60 minutes
35.0℃
35.0℃
34.4℃
34.4℃
7～8W