## Slide 1
Hiroshi Nakatsugawa1,*, Miwa Saito2, and Yoichi Okamoto3
1Yokohama National University, 79-5 Tokiwadai, Hodogaya-ku, Yokohama 240-8501, Japan
2Kanagawa University, 3-27-1 Rokkakubashi, Kanagawa-ku, Yokohama 221-8686, Japan
3National Defense Academy, 1-10-20 Hashirimizu, Yokosuka 239-8686, Japan
*e-mail of presenting author: naka@ynu.ac.jp
High temperature thermoelectric properties of perovskite type
Pr0.9Sr0.1Mn1-xFexO3 (0≦x≦1)
Notes: Thank you, Mr. Chairman.
Good morning everyone. Today, I’d like to talk about this title.
My name is Hiroshi Nakatsugawa from Yokohama National University, Japan.

## Slide 2: Outline
Introduction
Experimental procedure
Results and Discussion
  crystal structure
  magnetic susceptibility
  Heikes formula
  Electric resistivity
  thermopower
  Thermal conductivity and ZT
Summary
Notes: This slide shows the contents of my presentation.
First, I’m going to talk about Introduction.
Second, I want to explain Experimental procedure briefly.
Third, I’d like to talk about Results and Discussion.
Finally, I will summarize my talk.

## Slide 3: Introduction
Oxides which show high carrier density and high Seebeck coefficient
Oxides which show high carrier density in the conduction band
Oxides which show high electron mobility and high electric conductivity
CoO2 layer
CoO2 layer
Na layer
Block layer
NaxCoO2
[Ca2CoO3]0.62CoO2
Phys. Rev. B56, R12685 (1997)
Jpn.J.Appl.Phys. 39, L531 (2000)
Al doped ZnO
Perovskite-type oxides
Ca0.9Yb0.1MnO3
Ca0.96Bi0.04Mn0.96V0.04O3
J.Appl.Phys. 79, 1816 (1996)
J.Appl.Phys. 100, 084911 (2006)
Solid State Commun. 145, 132 (2008)
P-type thermoelectric oxides
Ｎ-type thermoelectric oxides
Notes: I’d like to start by talking about Introduction. Today, oxides are known as a possible candidate for thermoelectric materials at high temperature.
In the case of p-type thermoelectric oxides, layered cobalt oxides show high carrier density and high Seebeck coefficient. In the case of n-type thermoelectric oxides, aluminum doped zinc oxide shows high carrier density in the conduction band, and perovskite-type oxides show high electron mobility and high electric conductivity at high temperature.

## Slide 4: Introduction
CaMn0.98Mo0.02O3
(CaMnO3)
Ca2.7Bi0.3Co4O9
(Ca349)
Int.Appl.Ceram.Tech. 4, 535 (2007)
J.Am.Ceram.Soc. 87, 1952 (2004)
CaMnO3
Al2O3 plate
Ag ingot
Ca349
ηmax = 2%
Thermoelectric oxides module which consists of PN elements of small linear thermal expansion coefficient difference is desired.
perovskite-type oxides :
Pr0.9Sr0.1Mn1-xFexO3 (0≦x≦1)
Notes: In fact, Urata et al. have built thermoelectric modules consisting of layered cobalt oxide and perovskite-type oxide.
However, the n-type elements were damaged by thermal stress between the alumina substrate and the n-type element.
To overcome such a lack of oxide thermoelectric materials, thermoelectric module which consists of PN elements of small linear thermal expansion coefficient difference is desired. So, we have paid attention to perovskite-type oxides.
The purpose of this study is to investigate p-type thermoelectric properties of this materials.

## Slide 5: Experimental procedure
powder X-ray diffraction @RT
: RINT2500
Rietveld analysis
: RIETAN-FP program
χ ：5K - 350K @ H = 1T , MPMS
ρ ：dc four-probe method
S ：steady-state technique
κ = dCvα
d：Archimedes method @RT
Cv：differential scanning calorimetry@RT
α：laser flash method, TC-7000
イオン半径
(Å)
BVパラメーター
r0 (Å)
fabrication
determinaiton
Pr0.9Sr0.1Mn1-xFexO3 (0≦x≦1)
solid-state reaction method
stoichiometric mixture
calcined at 1000℃ in air
sintered at 1300℃ in O2
pressed into pellets
Notes: Now, I want to talk about Experimental procedure briefly. Polycrystalline samples were synthesized by using solid-sate reaction method.
Crystal structure parameters were studied by using Rietveld analysis of powder X-ray diffraction data. Magnetic susceptibility was measured by using MPMS below 350K under magnetic field of 1T. Electric resistivity was measured by using dc four-probe method, and Seebeck coefficient was measured by using steady-state technique. Thermal conductivity was measured from bulk density, specific heat, and thermal diffusivity. In particular, thermal diffusivity was measured by using laser flash method above room temperature.

## Slide 6
crystal structure
BVS = 3.13 (v.u.)
BVS = 2.89 (v.u.)
BVS = 3.07 (v.u.)
BVS = 2.97 (v.u.)
Pbnm
Pbnm
Fe-O1 : 1.995(Å)
Fe-O2 : 1.988(Å)
Fe-O2 : 1.996(Å)
Mn-O1 : 1.963(Å)
Mn-O2 : 1.939(Å)
Mn-O2 : 2.032(Å)
Jahn-Teller
distortion
Pr0.9Sr0.1Mn1-xFexO3 (0≦x≦1)
Notes: Next, I’d like to move on to Results and Discussion.
Firstly, I’d like to talk about crystal structure of praseodymium strontium manganese iron oxides.
X-ray diffraction data show that all samples are single phase and crystal structure is orthorhombic structure.
The bond valence sum of A site and B site was observed about 2.9 and 3.1which corresponds to a nominal ionic valence, respectively.
In particular, manganese rich samples were observed the Jahn-Teller octahedral distortion.

## Slide 7
magnetic susceptibility
Notes: This slide shows temperature dependence of magnetic susceptibility and inverse magnetic susceptibility
This figure shows ferromagnetism is suppressed with changing from manganese rich samples to iron rich samples.
On the other hand, the slope of the linear relation shows inverse Curie constant.
From Curie constant , we can obtain the effective magnetic moment and the spin quantum number of B site ions.

## Slide 8
Heikes formula
= 170μV/K
LS Fe3+
LS Fe4+
LS Fe3+
LS Fe3+
IS Fe3+
LS Fe4+
IS Fe3+
IS Fe3+
= 183μV/K
= 21μV/K
HS Mn3+
HS Mn3+
HS Mn3+
HS Mn4+
HS Mn3+
HS Mn3+
HS Mn3+
HS Mn3+
x = 0
x = 1
Notes: In the case of manganese rich sample of x = 0, the B site ions consist of high spin manganese trivalent and tetravalent ions.
The thermopower in the high temperature limit is estimated to be 170μV/K by using Heikes formula.
In the case of iron rich sample of x = 1, the B site ions consist of low spin iron trivalent, low spin iron tetravalent, and intermediate spin iron trivalent ions.
Therefore, the thermopower in the high temperature limit is estimated to be 204μV/K which corresponds to experimental value.

## Slide 9: electric resistivity
Notes: This slide shows temperature dependence of electric resistivity and Arrhenius relation of σT against inverse temperature.
All samples show a semiconducting behavior over the whole temperature range and resistivity increases with increasing x.
However, resistivity decrease rapidly as x increases from x = 0.9 to x = 1.
This means that low spin iron ions dominates the electric structure of the iron rich samples.
In addition, all samples show a small polaron behavior above room temperature.

## Slide 10: thermopower
Notes: This slide shows temperature dependence and inverse temperature dependence of thermopower.
All samples show a large positive thermopower below room temperature.
Above room temperature, the thermopower of manganese rich samples decrease gradually and approach zero.
On the other hand, the thermopower of iron rich samples keep large value and show a gradual increase.
In particular, the thermopower in the high temperature limit of iron rich samples is in good agreement with experimental values.

## Slide 11: thermal conductivity and ZT
Notes: This slide shows temperature dependence of thermal conductivity and ZT.
All samples show small thermal conductivity up to 2.5 W/mK over the whole temperature range.
Although electric thermal conductivity increase with increasing temperature, the influence is very small.
So lattice thermal conductivity is more important than electric thermal conductivity in this sample.
Clearly, the sample for x = 1 shows the largest ZT of 0.08 at 850K.
This indicates that hole-doped perovskite-type iron oxides show promising p-type thermoelectric properties at high temperature.

## Slide 12: Summary
With increasing x, the majority ions of B-site changes from HS Mn3+ and HS Mn4+ to LS Fe3+ and LS Fe4+. In particular, part of trivalent ions for x = 1 change from LS Fe3+ to IS Fe3+.
All the samples show a small polaron behavior above room temperature.
The positive S for x≧0.9 show a gradual increase up to 850K and the predicted S∞ defined by Heikes formula for x≧0.9 are in good agreement with experimental values.
The largest ZT value for x = 1 is 0.08 at 850K. This indicates that hole-doped perovskite-type Fe oxides show promising p-type thermoelectric properties at high temperature.
Notes: Conclusion is as follows. In conclusion,
with increasing x, the majority ions of B-site changes from HS Mn3+ and HS Mn4+ to LS Fe3+ and LS Fe4+. In particular, part of trivalent ions for x = 1 change from LS Fe3+ to IS Fe3+.
All the samples show a small polaron behavior above room temperature.
The positive S for x≧0.9 show a gradual increase up to 850K and the predicted S∞ defined by Heikes formula for x≧0.9 are in good agreement with experimental values.
The largest ZT value for x = 1 is 0.08 at 850K. This indicates that hole-doped perovskite-type Fe oxides show promising p-type thermoelectric properties at high temperature.

## Slide 13
Thank you for your attention.
Notes: Thank you for your attention.

## Slide 16
ions | ionic radius | bond valence parameter
La3+ | 1.36 | 2.172
Pr3+ | 1.179 | 2.138
Sr2+ | 1.44 | 2.118
Fe3+ | 0.645 | 1.751
Fe4+ | 0.585 | 1.765
Mn3+ | 0.645 | 1.732
Mn4+ | 0.53 | 1.750
O2- | 1.40 | －