## Slide 1
Masaki Kubota, Yosuke Watanabe, Hiroshi Nakatsugawa
Yokohama National University
Thermoelectric properties of n- and p-type polycrystalline Pr1-xSrxMnO3 (0.1≦x≦0.9)
Notes: Hallo, my name is Masaki Kubota. YNU student.
I belong to Nakatsugawa lab.
Today, I'm going to talk about thermoelectric properties of n- and p-type polycrystalline Pr1-xSrxMnO3(0.1≦x≦0.9).

## Slide 2
electron
holl
p-type
n-type
High temperature
Low temperature
電流
current
・p-type and n-type semiconductor joined series.
・Direct transformation in electric energy in thermal energy.
What is thermoelectric conversion ?
Introduction
The difference of thermal expansion rate causes the break of the element.
→ Want same element of p-type and n-type!
Fig. 2 Example of n-type thermoelectric materials broke in a process to repeat thermoelectric power generation
Fig. 1 Thermoelectric conversion module model.
Now hopeful Oxide thermoelectric materials
n-type： CaMnO3 (CaMn0.98Mo0.02O3)
p-type： layered cobalt oxide（Ca2.7Bi0.3Co4O9）
Notes: The first, Introduction of this study.
Do you know what is thermoelectric conversion?
The word of thermoelectric is consisted of thermal and electric. As its name suggests it effect interconversion thermal and electric.
In this study, focus on to the Seebeck effect which converts difference of temperature into electricity.
Look at this picture please.
This picture is n-type thermoelectric materials broke in a process to repeat thermoelectric power generation.
Why has it been broken?
It is the difference of thermal expansion rate causes the break of the material.
→ The p-type and n-type are used almost the same material, It’s way of solving!

## Slide 3
・Strongly correlated electron system
・ MnO6 octahedral is distorted by interaction of O site
→Often becomes the low symmetric tetragonal and orthorhombic crystal
Perovskite type Mn oxide
background
●：A site
●：Mn site
●：O site
Fig. 3 Perovskite type structure
eg orbit
t2g orbit
Five-fold
degeneration
・Degeneration is removed
・Crystalline field division energy is smaller than Hund’s binding energy, it is high spin.
Fig. 4 Mn3d orbit’s electronic state
Notes: In this study, we remark Perovskite type Mn oxide
Its characteristic is Strongly correlated electron system and its crystal’s MnO6 octahedral is distorted by interaction of O site
Its effect is often becomes the low symmetric tetragonal and orthorhombic crystal
Please look at this picture. This picture is the model that is in an electronic state of the Mn3d orbit
The 3d orbit which was retracted by shrinking to five folds of the Mn is affected by the crystalline field that oxygen forms in crystals, and degeneration comes loose.
The crystalline field division energy is about 1eV. It is smaller than フント-binding energy about 2eV, it become high spin state. (t2g3 eg1: S = 2)

## Slide 4
At the Strongly correlated electron system’s Seebeck coefficient is represented by Koshibae’s theory.
Mn3+ : g3
Mn4+ : g4
eg
eg
t2g
t2g
S=2
S=3/2
Spin degree of freedom ：5
S=2,1,0,-1,-2
Spin degree of freedom：4
S=3/2,1/2,-1/2,-3/2
Orbital degree of freedom：2
At Perovskite type Mn oxide
5×2
4×1
Spin degree of freedom × Orbital degree of freedom
Orbital degree of freedom：1
background
Notes: At the Strongly correlated electron system’s Seebeck coefficient is represented by Koshibae’s theory.
It is represented by this formula
At this formula, g3 and g4 is squared spin and Orbital’s digree of freedoms
It’s calculated almost 79μV/K

## Slide 5
research object
Mn4+ is caused by a change of the valence value, and carrier is introduced.
・Decrease Electrical resistivity
・Decrease Seebeck coefficient
Influence of the Sr dope to the Pr site in Pr1-xSrxMnO3
Pr, Sr
In this study…
I change Sr doped value of Pr1-xSrxMnO3 and examine composition indicating high thermoelectric properties in each domain of a p-type and the n-type to prevent the break of the module element by the difference in thermal expansion rate.
Notes: Research object
First, I show influence of the Sr dope to the Pr site of Pr1-xSrxMnO3
When Sr doped, Mn’s valence value is changing Mn3+ to Mn4+ and carrier is introduced.
Its effect is Decrease Electrical resistivity and lattice distorted.
In this study
I change Sr doped value of Pr1-xSrxMnO3 and examine composition indicating high thermoelectric properties in each domain of a p-type and the n-type to prevent the break of the module element by the difference in thermal expansion rate.

## Slide 6
（ ResiTest8300,80K～395K ）
（ ZEM-3, 373K～1073K ）
Powder X-ray diffraction （RINT2500, RT）
Thermal diffusivity （TC-7000-R, RT～970K）
Specific heat （DSC, 303K ~ 323K）
press
Weighing
Mixture
measurement
Starting material：Pr6O11, SrCO3, Mn2O3
Pr1-xSrxMnO3 (0.1≦x≦0.9)
Wet mixing （0.5 h）
1373 K, 24 h (at Air ×2）
Uniaxial pressing（18 MPa）
1673 K, 48 h ( at N2)
Electrical resistivity and Seebeck coefficient
Experimental
Calcine
Firing
Notes: Next is Experimental.
We have fabricated polycrystalline PrSrMnO3 using a solid-state reaction method.
And I measured their parameters.

## Slide 7
Lattice parameters
Crystal system : orthorhombic, Space group : Pnma (Vol. A, 62)
peseudo-cubic
Orthorhombic (P n m a)
Orthorhombic (P n m a)
Orthorhombic (P n m a)
Tetragonal (I 4/m c m)
Tetragonal (I 4/m c m)
Tetragonal (I 4/m c m)
Notes: Next is result and discussion.
Lattice parameters are shown this picture.
It is orthorhombic crystal in the domain where is with less than it of concentration X = 0.4.
And
It is tetragonal in the domain with more than of concentration X = 0.5.
Anisotropy dissolved with increase in quantity of Sr dope in the orthorhombic crystal domain

## Slide 8
Electrical resistivity ＆ Seebeck coefficient
Electrical resistivity and the value of Seebeck coefficient decrease with increase value of Sr dope
→ Effect of carrier introduction by dope of Sr conspicuously
● x=0.1
● x=0.2
● x=0.3
● x=0.4
● x=0.5
● x=0.6
● x=0.7
● x=0.9
Temperature (K)
Electrical resistivity (Ωcm)
● x=0.1
● x=0.2
● x=0.3
● x=0.4
● x=0.5
● x=0.6
● x=0.7
● x=0.9
Seebeck coefficient (μV/K)
Temperature (K)

## Slide 9
Power factor ＆Thermal conductivity
Calculated a thermal conductivity of RT, 570K, 770K and 970K.
Calculated power factor from
Seebeck coefficient and Electrical resistivity.
● x=0.1
● x=0.2
● x=0.3
● x=0.4
● x=0.5
● x=0.6
● x=0.7
● x=0.9
Κ (W/mK)
Temperature (K)
● x=0.1
● x=0.2
● x=0.3
● x=0.4
● x=0.5
● x=0.6
● x=0.7
● x=0.9
Power facor (S2/ρ)
Temperature (K)

## Slide 10
Figure of merit ZT
Calculated figure of merit ZT from power facter and thermal conductivity.
ZT
Temperature (K)
● x=0.1
● x=0.2
● x=0.3
● x=0.4
● x=0.5
● x=0.6
● x=0.7
● x=0.9

## Slide 11
conclusion
I was confirmed x=0.1~0.4 was orthorhombic crystal, and x=0.5~0.7 was tetragonal crystal from Rietveld Analysis.
The effect by the increase in quantity of Sr dope influenced a lattice distortion and the increase in carrier.
Electrical resistivity and Seebeck coefficient decreased with anisotropic cancellation and showed metallic behavior in domains more than x=0.3.
ZT was 0.005 in x = 0.1 at 473K in the p-type domain and 0.09 in x = 0.7 at 770K in the n-type domain.
The possibility that I could modularize composition indicating high performance by very near composition if provided was suggested at a more high temperature level with a p-type.

## Slide 12
Thank you for your kind attention.