## Slide 1
Yokohama National University*, National Defense Academy1), Chubu University2)
H.Nakatsugawa*, Y.Okamoto1), T.Kawahara2), S.Yamaguchi2)
Self-cooling on power MOSFET using copper plating single-crystalline silicon wafers
IUMRS-International Conference on Electronic Materials 2012
Sept.23 – 28, 2012 Pacifico Yokohama, Yokohama, Japan
Notes: Thank you Mr Chairman.
My name is Hiroshi Nakatsugawa from Yokohama National University.
It is my great honor to be invited such an opportunity.
Today, I’m going to talking about “Self-cooling on power MOSFET using copper plating single-crystalline silicon wafers”

## Slide 2: Introduction
Low Temp
Bi2Te3
Mid Temp
Mg2Si, MnSi1.75-γ
CoSb3
High Temp
NaxCoO2
Ca3Co4O9
CaMnO3
Low Temp
Mid Temp
High Temp
Silicon wafer
Notes: Thermoelectric generation is very important from a point view of waste heat utilization. In order to realize 10% of energy conversion efficiency, ZT value needs to be above 1.
This figure shows ZT values of thermoelectric materials.
In the low temperature, bismuth telluride has high ZT value.
In the middle temperature, silicide and skutterudite attract attention.
In the high temperature, single-crystalline oxides have high performance.
But ZT values of polycrystalline oxide and single-crystalline silicon are very low.

## Slide 3
polycrystalline oxide
・stable in High Temp
・waste heat utilization, emergency power source
single-crystalline silicon
・application of self-cooling device using high thermal conductivity
Notes: Polycrystalline oxide is stable in the high temperature, and shows low resistivity and high Seebeck coefficient.
So, polycrystalline oxide can be applied to waste heat utilization or emergency power source.
On the other hand, single-crystalline silicon shows low resistivity, high Seebeck coefficient, and low ZT value because of high thermal conductivity.
So, single-crystalline silicon is expected to be application of self-cooling device using high thermal conductivity.

## Slide 4: Purpose
thermoelectric generation
element
thermoelectric cooling
element
self-cooling device
heat release
load
source
n
n
p
p
MOSFET
polycrystalline oxide
single-crystalline silicon
heat release
Notes: The purpose of this study is to show application of thermoelectric generation for polycrystalline oxide and self-cooling device for single-crystalline silicon.

## Slide 5: ① self-cooling for single-crystalline silicon ② themoelectric generation for polycrystalline oxide
Notes: First of all, I’m going to talk about self-cooling for single-crystalline silicon.

## Slide 6: thermoelectric cooling
n
p
EF
heat absorption
n
VB
p
CB
CB
CB
VB
VB
current
current
electron
heat release
heat
release
heat
absorption
Notes: Thermoelectric cooling is realized by the cycle of Peltier heat absorption and heat release.
But high-current cannot be passed because of a large Joule heat.

## Slide 7: self-cooling
EF
EF
current
MOSFET
self-cooling
current
electron
CB
CB
VB
VB
heat release
heat release
heat
release
heat
release
heat
absorption
heat
absorption
Notes: On the other hand, self-cooling is realized by the thermal conduction and the Peltier heat absorption.
In this case, high-current can be passed because of a small Joule heat.

## Slide 8
Method
resistivity
thermoppwer
10mΩcm
3mΩcm
－200μV/K
193μV/K
Ti 0.1μm
Au 0.4μm
Sb doped n-type Si wafer
B doped p-type Si wafer
20mm
30mm
0.52mm thick
Si
Ti
Au
Cu
R = 0.087 mΩ @ RT
R = 0.026 mΩ @ RT
RI2 = 139 mW @ I = 40A
RI2 = 42 mW @ I = 40A
Gate-Source V: 10V, Drain-Source I: 40A
The temperature measurement using infrared thermography every 10 minutes in two hours
The voltage measurement between Drain and Source
carrier concentration
carrier mobility
Notes: The electrode was fabricated on both surfaces by coating titanium and gold sputtering and copper plating.
This figure shows experimental setup, where white arrow shows the electric current of 40A.
MOSFET and single-crystalline silicon was located between copper blocks.
The temperature measurement was carried out using infrared thermography every 10 minutes in two hours.
The voltage between Drain and Source was also measured.

## Slide 9: Results: MOSFET only (40A)
17.4℃±0.6℃
11.6℃±0.8℃
63mV
Joule heat from MOSFET 2.52W
temperature （℃)
pixel value
120min
temperature （℃)
0
15
30
line profile
temperature （℃)
0
15
30
line profile
upper side temperature: 21.3℃
lower side temperature: 9.4℃
internal temperature: 13.8℃
●
●
●
●
Notes: This is the result when MOSFET is located between upper and lower copper blocks.
The temperatures of top and bottom side of MOSFET are measured by using the line profile of the infrared thermography.

## Slide 10: Results: MOSFET+n-Si (40A)
17.4℃±0.6℃
11.6℃±0.8℃
63mV
Joule heat from MOSFET 2.52W
Joule heat from MOSFET 2.52W
118mV
0.14W
Peltier heat from n-Si 2.06W
172μV/K
16.6℃±0.4℃
10.9℃±0.6℃
Joule heat from n-Si
－0.8℃
－0.7℃
●
●
●
●
Notes: This is the result when MOSFET with n-type silicon is located between upper and lower copper blocks.
A small cooling effect can be found.
But this is in the experimental error.
So, we have tried to modify the experimental setup.

## Slide 11
Notes: The fin made of stainless-steel was exchanged for the fin made of copper.
Then, MOSFET and single-crystalline silicon were located between fin and heatsink directly.
In addition, the water temperature in the heatsink was maintained 2℃ by the cooling water circulation system with ice.

## Slide 12: Results: MOSFET only (40A)
16.4℃±0.4℃
9.5℃±0.4℃
temperature （℃)
0
15
30
line profile
temperature （℃)
Joule heat from MOSFET 1.84W
46mV
temperature （℃)
pixel value
0
15
line profile
upper side temperature: 20.6℃
lower side temperature: 7.5℃
internal temperature: 11.3℃
●
30
120min
●
●
●
Notes: This is the result when MOSFET is located between fin and heatsink.
The average temperatures of top and bottom side of MOSFET are 16.4℃ and 9.5℃.

## Slide 13: Results: MOSFET+n-Si (40A)
16.4℃±0.4℃
9.5℃±0.4℃
Joule heat from MOSFET 1.84W
46mV
Joule heat from MOSFET 1.84W
68mV
0.14W
Joule heat from n-Si
Peltier heat from n-Si 0.74W
62μV/K
14.5℃±0.4℃
8.0℃±0.5℃
－1.9℃
－1.5℃
●
●
●
●
Notes: This is the result when MOSFET with n-type silicon is located between fin and heatsink.
The average temperature of top side of MOSFET decreases 1.9℃.
And the average temperature of bottom side of MOSFET decreases 1.5℃.

## Slide 14: Results: MOSFET+p-Si (40A)
16.4℃±0.4℃
9.5℃±0.4℃
Joule heat from MOSFET 1.84W
46mV
Joule heat from MOSFET 1.84W
0.04W
Peltier heat from p-Si 0.56W
47μV/K
61mV
15.7℃±0.4℃
8.5℃±0.4℃
Joule heat from p-Si
－0.7℃
－1.0℃
●
●
●
●
Notes: This is the result when MOSFET with p-type silicon is located between fin and heatsink.
The average temperature of top side of MOSFET decreases 0.7℃.
And the average temperature of bottom side of MOSFET decreases 1℃.

## Slide 15: Results: MOSFET+n-Si+p-Si (40A)
16.4℃±0.4℃
9.5℃±0.4℃
Joule heat from MOSFET 1.84W
46mV
Joule heat from MOSFET 1.84W
70mV
0.18W
Joule heat from n-Si & p-Si
Peltier heat from n-Si & p-Si 0.78W
65μV/K
15.1℃±0.5℃
8.2℃±0.5℃
－1.3℃
－1.3℃
●
●
●
●
Notes: This is the result when MOSFET with n and p-type silicons is located between fin and heatsink.
The average temperature of top side of MOSFET decreases 1.3℃.
And the average temperature of bottom side of MOSFET also decreases 1.3℃.

## Slide 16
① self-cooling for single-crystalline silicon ② themoelectric generation for polycrystalline oxide
Notes: Next, I’m going to talk about thermoelectric generation for polycrystalline oxide.

## Slide 17: Method
n-type thermoelectric elements： Yb doped CaMnO3
p-type thermoelectric element： Y doped Ca3Co4O9
Mn3O4 + CaCO3 + Yb2O3
Co3O4 + CaCO3 + Y2O3
solid-state reaction: 1300℃ in air
Ca0.99Yb0.01MnO3
solid-state reaction: 920℃ in O2
[(Ca0.9Y0.1)2CoO3]0.62 CoO2
n-type
element
p-type
element
silver paste coating
n
n
p
p
p
n
silver sheet
cubic,
6mm on a side
annealed at 850℃ in air
silver paste coating
2 PN pair
thermoelectric module
serial connection
Notes: Ytterbium doped calcium manganese oxide was used for n-type thermoelectric element.
And yttrium doped calcium cobalt oxide was used for p-type thermoelectric element.
These elements were cut for cubic of 6mm on a side.
Silver paste coating thermoelectric elements were serial connected on silver sheet and annealed at 850℃ in air.
Then, we get 2 PN pair thermoelectric module.

## Slide 18: Results: temperature difference
line profile
Temperature (℃)
500
water cooled heatsink
TE module
heater : 500℃
Temperature (℃)
pixel value
0
TH=709K
TL=330K
water cooled heatsink
heater : 600℃
TE module
18℃
TH=709K
TL=330K
Temperature (℃)
0
250
500
⊿T=379K
line profile
Notes: The temperature difference was estimated 379K by using the line profile of the infrared thermography.

## Slide 19: Results: average r and S values
94.3mΩcm
54.7mΩcm
r = 0.51Ω
|S| = 842μV/K
149.5μV/K
－271.5μV/K
⊿T
⊿T
PN 2pairs
PN 2pairs
Notes: In the temperature range, the average internal resistance and Seebeck coefficient of the thermoelectric module are found 0.51Ω and 842μV/K, respectively.

## Slide 20: Results: power performance
r+R=0.82Ω
R=0.31Ω
⊿T=399K
34mW
≒379K
PN 2pairs
PN 1pair
Notes: This figure shows voltage-current line and current-power curve of the thermoelectric module.
From the open-circuit voltage, we can get the temperature difference 399K.
This is in good agreement with the value from infrared thermoraphy.
From maximum current, we can get the contact resistance 0.31Ω.
And maximum power is 34mW.
This means 17mW per PN pair.
In addition, energy conversion efficiency can be found 0.21%.

## Slide 21: Results: optimization of element size
5.6
0.82
6mm
6mm
6mm
p
n
6mm
6mm
6mm
PN 2pairs
Notes: If the element shape is cubic, the internal resistance is in inverse proportion to the element length and the contact resistance is in proportion to the element area.
So, the module resistance has minimum at the element length of 5.6mm.
Fortunately, the element size is in good shape.

## Slide 22: Conclusion
We try to show the application of the self-cooling device for single-crystalline silicon.
The self-cooling of top and bottom side of MOSFET with n-type and/or p-type Si can be found in the electric current of 40A.
We try to show the application of thermoelectric generation for polycrystalline oxide.
In the temperature difference 399K, the maximum power per PN pair can be found 17mW.
Notes: In conclusion,
・We try to show application of the self-cooling device for single-crystalline silicon.
・The self-cooling of top and bottom side of MOSFET with n-type and/or p-type Si can be found in the electric current of 40A.
・We try to show application of thermoelectric generation for polycrystalline oxide.
・In the temperature difference 399K, the maximum power per PN pair can be found 17mW.

## Slide 23
Thank you for your kind attention.
IUMRS-International Conference on Electronic Materials 2012
Sept.23 – 28, 2012 Pacifico Yokohama, Yokohama, Japan
Notes: Thank you for your kind attention.