## Slide 1
Improvement of thermoelectric properties of β-FeSi2 by Ni substitution
Sopheap Sam1, *, Hiroshi Nakatsugawa1, Yoichi Okamoto2
Yokohama National University, Japan
National Defense Academy, Japan
* E-mail: sam-sopheap-fh@ynu.jp
2022-July-20th

## Slide 2: Outline
Introduction
- Crystal and band structure FeSi2.
- Phase transition of FeSi2.
- Review of previous research.
- Improve TE performance of β-FeSi2 by Ni substitution.
2. Experimental method
- Fabrication and measurement.
3. Results and discussions
- Crystal structure and phase identification.
- Thermoelectric properties (Seebeck coefficient, electrical resistivity, thermal conductivity, and ZT).
4. Conclusions

## Slide 3
Crystal and band structure of each phase FeSi2
Orthorhombic β-phase
Tetragonal α-phase
Cubic ε-phase
Space group: P213
Space group: P4mmm
Space group: Cmce
R. Girlanda et al., J. Appl. Phys. 76, 2837 (1994)
S. J. Clark et al., Physical review B., 58,16 (1998)
Fe1
Fe2
Si1
Si2

## Slide 4
Phase transition diagram of FeSi2
The equilibrium phase diagram for the system Fe–Si by Piton and Fay. α-phase:FeSi2, β-phase:FeSi2, ε-phase:FeSi.
The β-FeSi2 based material is a promising candidate for thermoelectric (TE) application working at high temperatures due to:
Environmental friendliness
Good thermal stability
Strong oxidation resistance
Low cost.
[X. L. Du et al., Acs Applied Materials & Interfaces, 12, 12901-12909 (2020)]

## Slide 5
Review of previous research
S: Seebeck coefficient [V/K]
ρ: resistivity [Ω.m]
κ: thermal conductivity[W/m.K]
β-Fe1-yNiySi2
β-Fe0.99-yCo0.01NiySi2
Smax at Ni doping 0.01
J. Tani and H. Kido, Journal of Applied Physics, 84, 1408-1411 (1998).
H. Nagai et. al., Journal of the Japan Society of Powder and Powder Metallurgy, 41, 560-564, 1994.
ρ can be reduced due to an increase in carrier concentration.
S can be increased by Ni substitution probably due to a reduction in mobility.

## Slide 6
Improve TE performance of β-FeSi2 by Ni substitution
Resistivity (ρ) can be decreased by the increase in carrier density (nH) by Ni-doping due to the larger valence electron.
However, with increasing x, as decreasing the ρ, the |S| also decreases. Therefore, we need to find the optimum Ni doping to improve the TE of β-Fe1-xNixSi2.
Seebeck coefficient (S) :
large me*
small mh*
mobility
In β-FeSi2 (x=0), the Seebeck coefficient |S| decreases with increasing temperature because of the bipolar effect.
By Ni doping, Hall mobility μH decreases and |S| increases because of the majority carrier for electrons.

## Slide 7
Arc-melting (20g)
NC wire cut
7x7x1.5mm
Vacuum sealing in quartz tube
Heat treatment 1150 oC, 3h
Annealing
840 oC, 20h
Experimental method
Fabrication :
7x7x1.5mm
Furnace 1150 oC, 3h.
Furnace 840 oC, 20 h.
Measurement :
XRD by Smart Lab, Rigaku
Rietveld analysis by RIETEN-FP
Thermal conductivity by power efficiency measurement (PEM-2)
ZT calculated by above parameters
Carrier concentration and mobility at RT by ResiTest 8300
Resistivity and Seebeck coefficient by ResiTest 8300 and homemade apparatus
3D SEM VE-8800

## Slide 8
Crystal structure and phase identification by Rietveld analysis
By using Rietveld Analysis with the measured data of XRD, all samples were grown in single beta β phase crystal structure with Cmce space group (base-centered orthorhombic) after heat treatment 1150 oC 3 h and annealing 840 oC 20 h.
FeSi2
β-FeSi2
(221)
(312)
(331)
(202)
(422)
(242)
(602)
(533)
(515)
(024)
(112)
Si2
Si1
Fe2
Fe1
SEM images also verify with the XRD result for the single β-phase after heat treatment.

## Slide 9
Electrical resistivity (ρ) of β-Fe1-xNixSi2
x
nH
ρ
μH
ρ
The increase in nH contributes positively to the decrease in ρ.
The decrease in μH contributes negatively to the decrease in ρ.

## Slide 10
x
Seebeck coefficient (S) of β-Fe1-xNixSi2
x=0, bipolar effect deteriorates S due to a narrow band gap.
nH
|S|
The bipolar effect is reduced by Ni substitution

## Slide 11
Thermal conductivity (κ) and ZT of β-Fe1-xNixSi2
The κ of Ni doping samples is higher than that of non-doped samples probably due to an increase in nH.
ZTmax
The ZTmax = 0.019 is obtained in x = 0.001 sample due to the significant increase of S and also the decrease in resistivity. PF of x = 0.001 is about 70 times higher than that of x = 0.

## Slide 12
Conclusions
The electrical resistivity decreases with Ni doping level due to an increase in nH.
The Seebeck coefficient decrease with Ni doping level, where the highest value is obtained in x = 0.001 with the value of 450 μV/K at 450 – 500 K. Small doping amount is more effective.
The thermal conductivity slightly increases with Ni doping.
The highest ZT = 0.019 at 580-600 K is obtained in the x = 0.001 sample due to the significant increase in Seebeck coefficient and reduction in electrical resistivity.

## Slide 13
Authors | x | S [μV/K] | PF [μW/m.K2] | Fabrication method
M. Komabayashi et al. [1] at 300K | 0.06 | -113 | 17 | Thin film by RF sputtering
This study at 300K | 0.001 | -393 | 13 | Bulk +by arc melting
H. Nagai et al. [2] at 650K | 0.01 | -240 | 50 | Bulk by mechanical milling + hot-pressing
This study at 500K | 0.001 | - 450 | 280 | Bulk by arc melting
Comparison with previous reports for TE properties of Fe1-xNixSi2
[1] M. Komabayashi, K. Hijikata, and S. Ido, Jpn. J. Appl. Phys. 30, 331 (1991).
[2] H. Nagai, I. Maeda, S. Katsuyama, and K. Majima, Journal of the Japan Society of Powder and Powder Metallurgy, 41, 560-564, (1994).

## Slide 14: Thank you for your attention!

## Slide 15
TE properties of β-Fe1-xNixSi2 at RT
x | L𝚶 [V2/K2] | r | nH [1/cm3] | μH [cm2/V.s ] | ¦S¦ [μV/K] | ρ [Ω.cm] | κ [W/mK]
0 | 1.792×10-8 | -1/2 | 1.3(2)×1016 | 37(4) | 127 | 7.21(3) | 7.16
0.001 | 1.624×10-8 | -1/2 | 1.2(4)×1017 | 35(7) | 393 | 1.52(3) | 8.25
0.005 | 1.656×10-8 | -1/2 | 2.6(2) ×1017 | 34(3) | 194 | 0.69(1) | 8.57
0.010 | 1.648×10-8 | -1/2 | 3.2(7) ×1017 | 27(5) | 205 | 0.716(9) | 8.44
0.015 | 1.674×10-8 | -1/2 | 4.8(4) ×1017 | 20(1) | 176 | 0.629(5) | 7.27
0.02 | 1.766×10-8 | -1/2 | 1.2(4) ×1018 | 11(3) | 135 | 0.502(2) | 7.12
0.03 | 2.139×10-8 | -1/2 | 2.3(2) ×1018 | 10(1) | 62 | 0.26(2) | 6.18

## Slide 17
Bipolar
Bipolar effect remarkably dominate at low nH .
J. J. Gong et al., Physical Chemistry Chemical Physics,18, 16566-16574 (2016).