## Slide 1
Investigation of p-type thermoelectric properties for Mn doped β-FeSi2
Farooq Umar1, Sopheap Sam2, Rio Oshita1, and Hiroshi Nakatsugawa 1*
1Yokohama National University,
2National Institute for Materials Science
*E-mail: nakatsugawa-hiroshi-dx@ynu.ac.jp
Notes: ----- 会議メモ (15/09/12 14:28) -----

## Slide 2: Contents
Introduction
Experimental Methods
Results and Discussions
Conclusion

## Slide 3
Introduction

## Slide 4: Introduction
Thermoelectricity phenomenon of transforming heat into electricity
Driving force = heat flow by a Temp gradient
Based on n-type and p-type semiconductors
Loss of 70% of global energy = waste heat released into the environment without utilization.
Thermoelectric generators harvest electrical energy with the help of assembled thermoelectric elements
p
n
h+
e-
High Temp
Low Temp
Notes: Thermoelectricity is a physical phenomenon describing the direct transformation of heat into electricity without any moving parts.
Thermoelectric generators are devices to harvest electrical energy with the help of suitably assembled thermoelectric elements1).
The driving force behind thermoelectricity is a heat flow caused by a thermal gradient in a conductive material.
They are based on the pairs of n-type and p-type semiconductors connected to larger assemblies.
In practical thermoelectric generator or cooler, n-type and p-type thermoelectric elements are joined and arranged as a thermoelectric device.

## Slide 5
Introduction
Thermoelectric Materials
Nano Wires NWs
Carbon Nanotubes CNT
Selenides
Tellurides
Silicides
Magnesium Silicides
Iron Silicides
Mg2.15Si0.28Sn0.71Sb0.006
ZT of 1.3 at 700 K
Mechanically not reliable
Mg2.15Si0.28Sn0.71Sb0.006

## Slide 6: Phase Transition
Formation of β-FeSi2
Peritectoid reaction
α-Fe2Si5 + ε-FeSi β-FeSi2
Eutectoid decomposition of
α-Fe2Si5 β-FeSi2 and Si

## Slide 7: Crystal Structures
Iron Silicides phases
α-Fe2Si5
β-FeSi2
ε-FeSi
Metallic
Metallic
Semiconducting

## Slide 8: Objective of the Research
Investigating the effect of Mn doping for enhancing the ZT of
β-FeSi2.
Achieving high ZT,
S ρ, κ
In the case of Mn doped β-FeSi2
ρ ( n -1) carrier mobility (μ)
( μ -1)
carrier concentration (n)
S ( n -2/3)
Optimizing the level of doping
}
Drude’s formula
ρ = 1/ |e| μ n
Mott’s formula
ZT = S2 T/ρ κ
Notes: The purpose of this study is to investigates the effect of Co and Ni doping for enhancing the ZT of β-FeSi2.
To achieve high ZT, we need to increase the S of the material and decrease the ρ and κ.
But in the case of Co and Ni doped β-FeSi2 while decreasing the ρ, the carrier concentration (nH) increases which in turn reduces the S.
So, for this purpose, we are going to optimize the level of doping to achieve maximum S and lower ρ to achieve high ZT.

## Slide 9
Experimental Methods

## Slide 10: Experimental Methods
XRD
SEM
Hall Effect
Resistivity
Seebeck Coefficient
HT Measurement
Characterization Techniques
Thermal Conductivity
SEM-EDS
At 1423 K for 3 hr
At 1113 K for 20 hr
RIGAKU SmartLab
3D SEM VE 8800
Hitachi SU 8010
Homebuilt Apparatus up to 800 K
PEM-2 apparatus
ResiTest 8300 up to 395 K
At 300 K

## Slide 11
Results and Discussions

## Slide 12
SmartLab Rigaku with Cu Kα.
XRD data tallied ICSD database.
Metallic ε-phase at 2θ = 45.2o was observed along with β-phase.
Rietveld Analysis for the crystal parameters
(020)
(112)
(202)
(023)
(312)
(421)
(331)
(024)
(041)
(242)
(602)
(240
(533)
(515)
(202)
(422)
X-ray Diffraction for Fe1-xMnxSi2 (0 < x < 0.1)

## Slide 13
Non doped
Non-Annealed samples
SEM-EDS
SEM, SU8010, Hitachi
EDS XFlash5060FQ,
Bruker
Non doped
Annealed samples

## Slide 14
Mott’s formula
S n -2/3
Seebeck Coefficient
Pisarenko Graph
Good fitting occurs at m*= 0.5 ~ 2.5 me
Solid lines drawn by Mott’s formula
Circles and dots represents the experimental values
Notes: Seebeck Coefficient S was measured over the temperature range of 80-800K.
The original β-FeSi2 showed S was positive at 80-195K which indicate it as a p-type semiconductor while changing to n-type after 200K up to 800K.
The graph can be explained by the Mott’s formula S nH -2/3
Resistivity ρ of the sample was measured over the temperature range of 80-800K.
Drude’s formula explains the correlation between ρ and nH, ρ nH -1
Seebeck Coefficient S was measured over the temperature range of 80-800K.
The original β-FeSi2 showed S was positive at 80-195K which indicate it as a p-type semiconductor while changing to n-type after 200K up to 800K.
The graph can be explained by the Mott’s formula
𝑆=(𝑘_𝐵^2 𝑇)/(3|𝑒| ℏ^2 ) 𝑚∗[𝜋/𝑛_𝐻 ]^(2⁄3)
S ∝ nH -2/3
Resistivity ρ of the sample was measured over the temperature range of 80-800K.
Drude’s formula explains the correlation between ρ and nH,
ρ = 1/ |e| μH nH
ρ ∝ nH -1

## Slide 15
Drude’s formula
ρ = 1/ |e| μ n
ρ n -1
Electrical Conductivity
σ = 1/ ρ
σ n
Electrical Resistivity
Electrical Conductivity

## Slide 16: Power Factor PF
PF = S2/ ρ
PF of the doped samples increased compared to non -doped FeSi2.
Maximum PF for non-doped β-FeSi2 3.4 μWm-1K-2 at 450 K
Maximum PF for doped β-Fe0.97Mn0.03Si2 and 971 μWm-1K-2 at 800 K respectively.

## Slide 17: Thermal Conductivity
Thermal Conductivity κ
κ= κe + κl
Increased
Reason
Formation of Metallic Phase
Increase in Electronic thermal Conductivity
Electronic Thermal Conductivity κe
κe = L0ρ-1T
Wiedemann Franz law
Electrical Thermal Conductivity

## Slide 18: ZT Figure of Merit
ZT = S2 ρ-1 κ-1 T
=PF κ-1 T
For non-doped β-FeSi2
ZT = 0.00024 at 450K
Maximum ZT = 0.12 at 800K
for β-Fe0.97Mn0.03Si2
Notes: The Power Factor (PF) of the samples was calculated over the temperature range of 80-800K.
The formula which explains the data is as, PF = S2/ ρ
It is very much clear from the data that the PF of the doped samples increased with increasing temperature as compared to non doped FeSi2.
The dimensionless ZT figure merit for the samples was calculated over the temperature range of 80-800K.
The formula which explains the data is as,
ZT = S2 ρ-1 κ-1 T
=PF κ-1 T
It is very much clear from the data that the ZT of the doped samples increased with increasing temperature as compared to non doped β-FeSi2.
The maximum ZT achieved was 0.31 for Fe0.96Co0.02Ni0.02Si2

## Slide 19
Conclusion

## Slide 20
Summary
Samples for β-Fe1-xMnxSi2 (0 < x < 0.10) were synthesized by Arc Melting method followed by Heat Treatment at 1423 K for 3 hr and Annealing at 1113 K for 20 hr.
All samples were grown in single β-phase but still some traces for ε-phase were found at 2θ = 45.2o, which was confirmed by SEM and SEM-EDS images.
Semiconducting phase increases for β-Fe1-xMnxSi2 (0.05 < x < 0.10) and is higher than 95 % for all samples and is maximum at Fe0.96Mn0.04Si2 which is 98.86 %.
In samples of β-Fe1-xMnxSi2 (0 < x < 0.10) decrease in ρ occurred because of increase in carrier concentration while S was enhanced because of increase in effective mass.
Because of reduction in bipolar effect S becomes uniform at high temperature for β-Fe1-xMnxSi2 (0 < x < 0.10) samples as compared to β-FeSi2
Thermal Conductivity for all doped samples slightly increases in comparison to non doped samples.
Throughout the study maximum Power factor was achieved for β-Fe0.97Mn0.03Si2 which is 971 μ Wm-1K-2 while highest ZT was found to be 0.12 for β-Fe0.97Mn0.03Si2 at 800 K.

## Slide 21
Thank you
for your kind attention