## Slide 1
Experimental
Thermoelectric properties of Sm1-xCaxFeO3-δ (0.1≦x≦0.8) and
Ho1-xCaxFeO3-δ (0.1≦x≦0.9) perovskite-type oxides
Hiroshi Nakatsugawa1※, Muhammad Ibrar1, Fumiya Konishi1, Koichi Kitahara2
1Yokohama National University (Yokohama 240-8501 Japan), 2 National Defense Academy (Yokosuka 239-8686 Japan)
※E-mail : nakatsugawa-hiroshi-dx@ynu.ac.jp TEL : +81-45-339-3854
Introduction
TE generation
Acknowledgments : Part of this research experiment was conducted using equipments at the Institute for Solid State Physics, University of Tokyo,
National Defense Academy, and the Instrumental Analysis and Evaluation Center, Yokohama National University.
Conclusion
Seebeck coefficient S
熱伝導率
Focusing on transition metal iron oxides with a perovskite structure, we aim to develop TE oxides that exhibit both P-type and N-type behavior with the same composition.
Rietveld analyses for XRD data
magnetic susceptibility χ
Sm1-xCaxFeO3-δ has a stable orthorhombic perovskite structure when x ≤ 0.5, but the perovskite structure is not maintained when x ≥ 0.6 due to oxygen deficiency. Since the distortion of the FeO6 octahedra is small, the spin state of the Fe sites is LSFe3+1-xLSFe4+x or ISFe3+1-xLSFe4+x. As x increases, the Seebeck coefficient decreases, and consequently, ZT also decreases with increasing x, reaching a maximum ZT = 0.011 for x = 0.1 @ 600 K.
Ho1-xCaxFeO3-δ exhibits a stable orthorhombic perovskite structure at x ≤ 0.5, but at x ≥ 0.6, the perovskite structure is not maintained due to increased distortion of the FeO₆ octahedra. Due to the large distortion of the FeO₆ octahedra, the spin state of the Fe sites is HSFe3+1-xHSFe4+x. As x increases, the Seebeck coefficient remains constant, ZT also maintains a high value, reaching a maximum ZT = 0.014 for x = 0.1 @ 600K.
Finding an n-type Fe transition metal oxide that maintains the orthorhombic perovskite structure even at x ≥ 0.6 and exhibits ZT = 0.01 @ 600 K is a future challenge.
Results & Discussion
The 41st International and 7th Asian Conference on Thermoelectrics (ICT/ACT 2025) on June 15-19, Sendai, Japan
TE cooling
XRD ： space group Pnma (No.62, D2h16)
Curie-Weiss law：
energy conversion efficiency
coefficient of performance
Oxides thermoelectric materials
ηmax = 2%
Int.Appl.Ceram.Tech. 4, 535 (2007)
Ca2.7Bi0.3Co4O9
(Ca349)
CaMn0.98Mo0.02O3
(CaMnO3)
Oxide thermoelectric materials that exhibit excellent performance in both P-type and N-type configurations exist, but there are no oxide TE conversion materials that exhibit both P-type and N-type performance with the same composition.
Chemically stable in oxidizing high-temperature
Composed of elements that are abundant on earth
Does not contain toxic elements
Maintenance-free and can be used for long time
Simple structure, resistant to vibration and impact
●Advantages
●Disadvantages
●Research purpose
tolerance factor：
1000℃ 24h
in air
1200℃ 48h
in O2
A (Sm3+, Ho3+, Ca2+)
O2-
P-180
Heikes formula
S∞ for A1-xCaxFe3+1-xFe4+xO3-δ (δ = 0)
LS Fe3+1-x LS Fe4+x
IS Fe3+1-x LS Fe4+x
HS Fe3+1-x HS Fe4+x
figure of merit ZT
thermal conductivity κ
electric resistivity ρ
(101)
(101)
(020)
(020)
(111)
(111)
(200)
(200)
(121)
(121)
(002)
(002)
(210)
(210)
(131)
(131)
(221)
(221)
(202)
(202)
(040)
(040)
(230)
(230)
(212)
(212)
(321)
(311)
(311)
(321)
(240)
(240)
(042)
(042)
(123)
(123)
(410)
(410)
(242)
(242)
Sm0.5Ca0.5FeO3-δ
Ho0.5Ca0.5FeO3-δ
crystal field splitting
perovskite structure : ABO3 (t = 1)
B (LS Fe3+, IS Fe3+, HS Fe3+,
LS Fe4+, HS Fe4+)
crystal field splitting : Small or Middle
Small
Small
Middle
Large
Large
crystal field splitting :Large
O1
O1
O2
O2
Sm0.5Ca0.5
Ho0.5Ca0.5
Fe
Fe
1.40Å
1.24Å
1.07Å
1.34Å
crystal field splitting：Large
crystal field splitting：Small
Weighing
mixing
pre-firing
crushing
mixing
press
forming
sintering
Powder
XRD
Rietveld analyses
Electric resistivity ρ
Seebeck coefficient S
Thermal conductivity κ
Magnetic susceptibility χ
Evaluation of ZT
Samples with x ≥ 0.6 show advanced oxygen deficiency and cannot maintain the Pnma perovskite structure.
Samples with x ≥ 0.6 show increased octahedral distortion and cannot maintain the Pnma perovskite structure.
LS Fe3+1-x LS Fe4+x or
IS Fe3+1-x LS Fe4+x
HS Fe3+1-x HS Fe4+x
s = 2.5
s = 2.0
s = 1.0
s = 0.5
s = 1.5
s = 1.0