## Slide 1
Design for Thermoelectric (TE) Materials
  High dimensionless figure of merit (ZT)
  Low toxicity, Low cost, Practical
Characteristics of half-Heusler alloys TiNiSn
  N-type thermoelectric material
  High power factor (Wm-1K-2)
  Chemically stable at high temperature (≤ 1273 K)
What we have found so far
  More than 3% Co substitution at Ni-site makes P-type*
  Low ZT compared to N-type (≈0.3)
  ⇒ Focus on intrinsic defects (interstitial Ni atoms)
What effect decreasing defects have on TE properties Hole carrier density increases due to decrease of interstitial Ni atoms as donor impurity. As a result, electrical resistivity (ρ) decreases.
The 41st International and 7th Asian Conference on Thermoelectrics (ICT/ACT 2025)
June 15-19, 2025, Sendai, JAPAN
P-type thermoelectric properties of half-Heusler alloys TiNi1-x-yCoySn (0≤x≤0.1, 0≤y≤0.05) below 800 K
Kosuke Yamazaki1, Sopheap Sam2, Hiroshi Nakatsugawa1* *E-mail : nakatsugawa-hiroshi-dx@ynu.ac.jp
1 Yokohama Natl. Univ., 79-5 Tokiwadai, Hodogaya, Yokohama, Kanagawa 240-8501, (Japan)
2 National Institute for Materials Science Namiki 1-1, Tsukuba, Ibaraki 305-0044, (Japan)
  Crystal structure
    XRD (Cu Kα : λ=1.5418 Å, SmartLab, Rigaku Holdings Co. )
    Rietveld analysis (RIETAN-FP)
  Chemical composition
    ICP-OES (ICPE-9000, SHIMADZU Co. )
    SEM-EDS (SU8010, Hitachi High-Tech Co.)
  Hall measurements
    300 K (ResiTest8300, TOYO Co. )
  Seebeck coefficient, Electrical resistivity
    80-395 K (ResiTest8300, TOYO Co. )
    395-800 K (Home-built apparatus)
  Thermal conductivity
    300-800 K (PEM-2, ULVAC, Inc. )
Sample preparation
Characterization method
P-153
Experimental method
Introduction
Thermoelectric properties & Electrical transport properties
Composition analysis
Conclusion
The crystal structure analysis shows that the interstitial Ni atoms decrease after the Ni composition ratio decrease. Thermoelectric properties show that the interstitial Ni atoms slightly decreasing is effective to improve ZT.
The maximum ZT (TiNi0.92Co0.05Sn) is attributed to the significant decrease of ρ and the maintenance of |S|. To further increase ZT, a reduction of κ is effective.
This results show that carrier density can be optimized by a simple method of reducing Ni composition, which is applicable to similar half-Heusler alloys.
In the future, we plan to reduce lattice thermal conductivity (κₗₐₜ) by doping with heavy elements to further increase ZT.
Acknowledgments: SmartLab, ICPE-9000 and SU8010 in this study were performed at the Instrumental Analysis Center, Yokohama National University. PEM-2 was performed at National Defense Academy of Japan.
Objective
The effects of reducing interstitial Ni atoms on the crystal structure, thermoelectric properties, and the ZT values of TiNi1-x-yCoySn (0≤x≤0.1, 0≤y≤0.05) are clarified.
Arc melting
Wire cutting
Annealing
Weighing
7 × 7 × 1 mm3 (ρ, S)
7 × 7 × 2 mm3 (κ)
1073 K, 168h
x y | 0.01 | 0.03 | 0.05
0 | ○ | ○ | ○
0.01 | - | - | ○
0.03 | - | - | ○
0.05 | ○ | ○ | ○
0.08 | - | - | ○
0.1 | ○ | ○ | ○
Vacuum pump
TiNi1-x-yCoySn
(0≤x≤0.1, 0≤y≤0.05)
：Seebeck coefficient (VK-1)
：Electrical resistivity (Ωm)
：Thermal conductivity (Wm-1K-1)
：Average Temperature (K)
S
ρ
κ
T
ΔT
P-type
N-type
Sample composition | Actual Sample composition
TiNiSn | Ti1.01Ni1.03Sn0.96
TiNi0.95Co0.05Sn | Ti1.00Ni0.99Co0.05Sn0.96
TiNi0.94Co0.05Sn | Ti1.02Ni0.94Co0.05Sn0.98
TiNi0.92Co0.05Sn | Ti1.02Ni0.95Co0.05Sn0.96
TiNi0.90Co0.05Sn | Ti1.02Ni0.93Co0.05Sn0.95
TiNi0.87Co0.05Sn | Ti1.01Ni0.90Co0.05Sn0.97
TiNi0.85Co0.05Sn | Ti1.02Ni0.89Co0.05Sn0.95
XRD pattern
Rietveld analysis
The indexed peaks in the figure are the peaks of the HH structure. The peaks were observed in all samples, indicating that the prepared samples are composed of HH phase.
Sample composition | ZT | T (K)
HfNi0.85Co0.15Sn* | ~0.3 | 700
TiNi0.92Co0.05Sn | 0.18 | 700
ZrNi0.98Co0.02Sn** | ~0.08 | 700
** Xie, H.-H. et al. J. Electron. Mater. 41, 1826 (2012).
* Ai, X. et al. Adv. Funct. Mater. 33, 2305582(2023) .
… ρ ∝ n-1, µ-1
… |S| ∝ m*, n-2/3
Rwp | 2.570
Re | 1.371
S | 1.874
RB | 3.773
RF | 1.943
(No. 216)
* Yamazaki, K. et al. Solid State Sci. 157, 107708(2024) .
e-
h+
h+
h+
h+
e-
e-
e-
h+
h+
h+
h+
The lattice constants and 4d site occupancy (interstitial Ni atoms) decrease with the reduction in Ni composition, suggesting a decrease in resistivity.
For x > 0.05, the mass fraction of the main phase decreases while the impurity phase increases, suggesting a deterioration in the thermoelectric properties.
ZT increase because the resistivity decrease.
Increase in hole carrier density due to decrease in interstitial Ni atoms.
The reduction of interstitial Ni atoms modifies the electronic structure in a way that enhances the Seebeck coefficient.
ZTmax=0.18 (T=700 K)
Ti | 4a | (0, 0, 0)
Ni | 4c | (¼, ¼, ¼)
Sn | 4b | (½, ½, ½)
Vacancy (Vc) | 4d | (¾, ¾, ¾)
TiNi0.85Co0.05Sn
Regions exhibiting strong Sn intensity are attributed to the presence of Ti6Sn5 and Sn, as identified by XRD.
All the samples exhibit compositions close to the nominal values, with the Ni content decreasing as x increases, as confirmed by ICP-OES.
Interstitial Ni atoms decrease
【Why does ρ decrease, yet |S| remains unchanged?】
Mott’s formula